## Slide 1: Removing Diffraction from X-ray Fluorescence Spectra for HfO2 Thin Film Characterization
Sonia Ghoshal
Mentor: Dr. Donald Windover
Div 643, Group 02

## Slide 2: Motivation: Transistors
Source
Drain
Gate
Gate oxide (HfO2)
p-type substrate (Si)
n+
n+
n-channel

## Slide 3: Goal
Assess the qualities of HfO2 films from manufacturers (thickness, impurities, elemental composition)

## Slide 4: Tool: Micro-X-ray Fluorescence
x-ray source
x-ray beam
detector
sample
fluorescence
“fingerprint”
XRF Spectra
= Tells us what elements are in a sample

## Slide 5: Problem: Diffraction
Light passing through a small slit scatters
  = diffraction
Si lattice spacing  diffraction peaks
Diffraction peaks!

## Slide 6: How do we remove diffraction?
rotate the sample
use software
apply filters

## Slide 7: 1) Filters
Thin sheets of Al, Ti, Cu
Purpose: decrease background radiation
TRADEOFF: removing noise at the expense of losing the actual signal
Findings: effective at reducing noise, but reduced Hf counts too much
x-ray source
x-ray beam
detector
sample

## Slide 8: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Discovered that 40-45 degrees allows for the best separation of diffraction and fluorescence peaks
0°:

## Slide 9: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Discovered that 40-45 degrees allows for the best separation of diffraction and fluorescence peaks
20°:

## Slide 10: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Discovered that 40-45 degrees allows for the best separation of diffraction and fluorescence peaks
40°:

## Slide 11: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Discovered that 40-45 degrees allows for the best separation of diffraction and fluorescence peaks
60°:

## Slide 12: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Findings: 40°- 45°allows for the best separation of diffraction and fluorescence peaks
80°:

## Slide 13: 2) Rotation
Rotating the chip in the XY plane changes the diffraction pattern observed
Discovered that 40-45 degrees allows for the best separation of diffraction and fluorescence peaks
40°: best angle!

## Slide 14: 3) Using software:
Used PyMca software to model the true fluorescence peaks versus the background radiation
Hf

## Slide 15: Finding the best fit:
Tested parameters to find the best fit
lower SNIP widths  more accurate fits
TRADEOFF: removing noise at the expense of losing the actual signal
Hf

## Slide 16: Computationally removing diffraction:
Removed background radiation to isolate the true fluorescence peaks
Findings: found a set of parameters (SNIP 10) that cleans up majority of diffraction while retaining Hf counts
Hf

## Slide 17: Recap
Rotating chip to ~ 40°- 45°, then using PyMca software with determined set of parameters allows for the removal of most of the diffraction and retainment of Hf counts
Hf

## Slide 18: Questions?